## Slide 1: Design and Engineering of Antibody Fragments for Sensitive Immuno-diagnostics
Japan-China Symposium on Chemical Engineering, March 17th, 2023
Yoichi Kumada
Associate Professor, Biochemical Engineering Lab,
Department of Functional Chemistry,
Kyoto Institute of Technology

## Slide 2: Design and development of interactive bio-material interface
Function of biomolecule
Catalysis (Enzyme)
Recognition (Ab, Receptor)
Materials
Organic
Inorganic
Hybrid
New bio-interface application
Artificial organs
Diagnostic substrate
Biocatalyst
Anti-microbial agent
Affinity separation
＋
Subjects to be solved by engineers
（Cost, Stability, Performance・・・）
immobilization
Solid materials
Proteins（Natural resources）

## Slide 3
Antibody-immobilized solid supports for immuno-diagnostics and bioprocess
Antibody
150,000 Da
Lateral-flow immunoassay
(Nitrocellulose membrane)
ELISA
（Flat polystyrene plate）
SPR sensor
(Gold thin layer)
Latex agglutination assay
(Non-porous PS latex beads)

## Slide 4
Monoclonal antibody is hetero-tetramer
Conventional antibody (whole Ab)
(150 kDa)
Heavy chain genes
Light chain genes
Gene expression
Translation
Folding
Post-translational modification
Assembly
Host cell: Hybridoma, CHO, HEK293
(Optional: animals)
Product

## Slide 5
Formation of single-chain Fv antibodies
Fusion protein that VH and VL genes were genetically connected.
Gene expression
Translation
Folding
Post-translational modification
Assembly
Host cell: Any
(Ex. E.coli)
Product
Single-chain Fv (scFv)
(30 kDa)

## Slide 6
Advantages of single-chain Fv antibodies in diagnosis
whole Ab
(150 kDa)
scFv
(30 kDa)
Advantages
・Small (20% size)
・Easy production
・Cheap (10% cost)
・High solubility
・Comparable affinity
・Any animal resources
・No ethical issues
VS

## Slide 7: Characteristics of immobilized antibodies （Ideal and real)
Evolution of molecular recognition
by antibody engineering
Ideal
・Dense
・Standing
・Active
Real
・Sparse
・Laying down
・Inactivated
Our Goal
・Denser!
・Uniform!
・Super active!

## Slide 8
Today’s topics
・ Isolation and characterization of rabbit single-chain Fv antibodies
・ Isolation and characterization of Materials-binding peptides
・ Site-specific immobilization of tagged scFvs for sensitive immuno-diagnostics

## Slide 9: Screening strategy for rabbit scFvs for bioanalysis
Antigen injection
scFv library preparation
（107 ～109 clones）
Phage library preparation
（ 1011 ～1013 phages）
Biopaninng
（109 → 102 clones）
Selection of positive clones
（102～ 103 clones）
Analysis of AA seq.
（102～ 103 clones）
Binding analysis
（102～ 103 clones）
Determination of koff
（102～ 103 clones）
Identification of candidates
（～10 clones）
Production check
（～10 clones）
Affinity & specificity check
（～10 clones）
Binding activity in
immobilization state
（～10 clones）

## Slide 10: Strategy for isolation of antibody fragments suitable for immunodiagnsis
 | Conventional method | Our original method
① Animal for immunization | Mouse （Low affinity） | Rabbit (Alpaca) （High affinity）
② Solid support for antigen immobilization | Plastic tube or beads | Liposomes （MLVs）
③ Characterization | ELISA, SPR AA seq | ELISA, SPR AA seq（CDR H3） Dissociation rate constant, koff
④ Selection strategy | affinity | Variety and stability
⑤ Evaluation | Performance in a liquid | Performance on a surface

## Slide 11: Ranking of scFv clones based on koff value
Round 2 or 3
Amino acid seq
ELISA
koff
CDR H3

## Slide 12
Chart: Rank 1 - Rank 5

## Slide 13
Chart: Rank 55 - Rank 60
scFv clones with higher koff values dissociated quickly during washing step.

## Slide 14: Dissociation constants of scFvs selected
sample name | kon(1/Ms) | koff(1/s) | Kd (M)
① R2-6 (Rank 7) | 6.09×104 | 2.66×10-5 | 4.37×10-10
② R2-7 (Rank 5) | Failed | Failed | Failed
③ R2-45 (Rank 10) | 1.52×104 | 5.16×10-5 | 3.39×10-9
④ R3-02 (Rank 8) | 4.70×104 | 1.92×10-4 | 4.07×10-9
⑤ R3-19 (Rank 3) | 4.16×104 | 9.02×10-5 | 2.17×10-9
⑥ R3-40 (Rank 1) | 2.34×105 | 2.84×10-6 | 1.21×10-11
SDS-PAGE （After IMAC）
Affinty determination by Biacore
Most of scFvs selected were successfully produced in recombinant E. coli cells, and those Kd values were ranged between 10-9～10-11 M.

## Slide 15: Different properties of rabbit and mouse scFvs
Chart: isoelectric point, -
Chart: isoelectric point, -
Rabbit scFvs hold different features such as pIs, compared with the mouse scFvs.
They might be more thermostable for application.

## Slide 16
Large-scale production of rabbit scFvs by fed-batch cultrure
ON-OFF signal
Notes: This slide shows the experimental set-up for fed-batch culture based on DO-stat strategy.
Dissolved oxygen, DO in a fermentor was measured by a probe-type DO sensor and the data was sent to PC through local controller. When the DO in a fermentor exceeds a set-value, for example 40%, a pump is active to start feeding.
Also, when DO value become lower than the set-value, the feeding pump is stopped. By repeating this operation, DO in a fermentor can be maintained at almost constant value.

## Slide 17
Time courses of fed-batch culture for anti-huIgG scFv (rabbit) production (strain No. 4 (+pelB reader)、DO=40%)
Production of scFv in culture supernatant by fed-batch culture
Notes: Then, we conducted the same experiment using different scFv strain, anti-human IgG scFv from rabbit (No.4). I mean different scFv sequences with different antigen-specificity.
As you can see here, quite similar tendency of results was obtained. I mean, insoluble scFv was expressed first with cell growth, and then, soluble scFv was released in culture supernatant and the final concentration was 3.1 g/L.

## Slide 18: Study on antibody immobilization for diagnosis
High selectivity
High affinity
Low-cost production
≠
High stability after immobilization
（High affinity, High capacity and High stability）
ELISA
SPR
Immuno-chromatography
Latex aggregation
CLEIA
usually evaluated during antibody screening
PS microplate
CM-dextran
Nitro-cellurose
PS latex beads
Magnetic beads
Not evaluated so far

## Slide 19
Today’s topics
・ Isolation and characterization of rabbit single-chain Fv antibodies
・ Isolation and characterization of Materials-binding peptides
・ Site-specific immobilization of tagged scFvs for sensitive immuno-diagnostics

## Slide 20: Materials-binding peptides (PS-tag, PC-tag, PMMA-tag, PDMS-tag, SiN-tag)
PS-tag (PCT/JP2009/000555)
PS19: RAFIASRRIKRP
PS19-4: RAIARRIRR
PS19-6: RIIIRRIRR
KPS19R10： KRAFIASRRIRRP
Material-binding peptide
Solid material
Functional protein
Advantage of material-binding peptides
Direct immobilization of protein with high density
Maintaining high remaining activity of protein after immobilization
Controlling orientation of protein uniformly
PC-tag (JP2010-031668)
PC-MLT8: WTPIMSTVMEIGYDNVESQR
PC-OMP6: NSNFFGLVDGLNFAVQYLGK
PMMA-tag (JP2010-031668)
PM-OMP25:DVEGIGDVDLVNYFEVGATYTFNK
SiN-tag (JP2012-028681)
ELN-TP14, ELN-CT22, ELN-V821
PDMS-tag (JP2015-026489)
ELN-V81, TPA-V81, OMC-V81

## Slide 21: Screening strategy of materials-binding peptide
Primary screening（Identification of material-binding proteins）
Secondary screening（Identification and evaluation of material-binding peptides）

## Slide 22: Glutathione S-Transferase (GST)
Aminoacid Sequence of GST
MSPILGYWKIKGLVQPTRLLLEYLEEKYEEHLYERDEGDKWRNKKFELGLEFPNLPYYIDGDVKLTQSMAIIRYIADKHNMLGGCPKERAEISMLEGAVLDIRYGVSRIAYSKDFETLKVDFLSKLPEMLKMFEDRLCHKTYLNGDHVTHPDFMLYDALDVVLYMDPMCLDAFPKLVCFKKRIEAIPQIDKYLKSSKYIAWPLQGWQATFGGGDHPPKSDLIEGRGIPGNSS
Materials-binding peptide candidates were introduced at C-terminus of the model enzyme, GST
C-terminus
N-terminus

## Slide 23: Glutathione S-Transferase (GST)
Aminoacid Sequence of GST
MSPILGYWKIKGLVQPTRLLLEYLEEKYEEHLYERDEGDKWRNKKFELGLEFPNLPYYIDGDVKLTQSMAIIRYIADKHNMLGGCPKERAEISMLEGAVLDIRYGVSRIAYSKDFETLKVDFLSKLPEMLKMFEDRLCHKTYLNGDHVTHPDFMLYDALDVVLYMDPMCLDAFPKLVCFKKRIEAIPQIDKYLKSSKYIAWPLQGWQATFGGGDHPPKSDLIEGRGIPGNSS
PS-tag: RIIIRRIRR
C-terminus
N-terminus

## Slide 24: Immobilization of GST-PS-tag to the surface of PS
Quartz Crystal Microbalance (QCM)
Frequency decreases by adsorption of protein
PS-tag-fused GST vs phi-PS
PS-tag-fused GST quickly bound to the PS surface.

## Slide 25: Glutathione S-Transferase (GST)
Aminoacid Sequence of GST
MSPILGYWKIKGLVQPTRLLLEYLEEKYEEHLYERDEGDKWRNKKFELGLEFPNLPYYIDGDVKLTQSMAIIRYIADKHNMLGGCPKERAEISMLEGAVLDIRYGVSRIAYSKDFETLKVDFLSKLPEMLKMFEDRLCHKTYLNGDHVTHPDFMLYDALDVVLYMDPMCLDAFPKLVCFKKRIEAIPQIDKYLKSSKYIAWPLQGWQATFGGGDHPPKSDLIEGRGIPGNSS
PC-tag: NSNFFGLVDGLNFAVQYLGK
C-terminus
N-terminus

## Slide 26
PC-tag-fused GST vs PC
Quartz Crystal Microbalance (QCM)
Immobilization of GST-PC-tag to the surface of PC
Frequency decreases by adsorption of protein

## Slide 27: Glutathione S-Transferase (GST)
Aminoacid Sequence of GST
MSPILGYWKIKGLVQPTRLLLEYLEEKYEEHLYERDEGDKWRNKKFELGLEFPNLPYYIDGDVKLTQSMAIIRYIADKHNMLGGCPKERAEISMLEGAVLDIRYGVSRIAYSKDFETLKVDFLSKLPEMLKMFEDRLCHKTYLNGDHVTHPDFMLYDALDVVLYMDPMCLDAFPKLVCFKKRIEAIPQIDKYLKSSKYIAWPLQGWQATFGGGDHPPKSDLIEGRGIPGNSS
PMMA-tag: DVEGIGDVDLVNYFEVGATYTFNK
C-terminus
N-terminus

## Slide 28
PMMA-tag-fused GST vs PMMA
Quartz Crystal Microbalance (QCM)
Immobilization of GST-PM-tag to the surface of PMMA
Frequency decreases by adsorption of protein

## Slide 29: Maximum density and dissociation constant (KD) of material-binding peptides
Name | Polymer | Maximum density (ng/cm2) | Dissociation constant (nM)
wt-GST | PC | 24 | ―
GST-PC-tag | PC | 830 | 73
wt-GST | PMMA | 77 | ―
GST-PM-tag | PMMA | 610 | 16
wt-GST | phi-PS | 21 | ―
GST-PS-tag | phi-PS | 670 | 86
By introducing materials-binding peptides, target proteins can be immobilized at high levels of density and affinity.

## Slide 30: Immobilization of GST onto the PS surface through PS-tag
Remaining activities
Adsorption Isotherm
Adsorbent: PS latex beads (Mean diameter; 1.0 mm)
Notes: This figure shows adsorption isotherm of wild-type GST, GST-PS19 and GST-PS23. Both PS-tag-fused GST showed much higher binding affinities and binding capacities. And as shown here, 10 times higher specific activities of GST on the PS latex beads were obtained.

## Slide 31: Materials-binding peptides (PS-tag, PC-tag, PMMA-tag, PDMS-tag, SiN-tag)
PS-tag (PCT/JP2009/000555)
PS19: RAFIASRRIKRP
PS19-4: RAIARRIRR
PS19-6: RIIIRRIRR
KPS19R10： KRAFIASRRIRRP
Material-binding peptide
Solid material
Functional protein
Advantage of material-binding peptides
Direct immobilization of protein with high density
Maintaining high remaining activity of protein after immobilization
Controlling orientation of protein uniformly
PC-tag (JP2010-031668)
PC-MLT8: WTPIMSTVMEIGYDNVESQR
PC-OMP6: NSNFFGLVDGLNFAVQYLGK
PMMA-tag (JP2010-031668)
PM-OMP25:DVEGIGDVDLVNYFEVGATYTFNK
SiN-tag (JP2012-028681)
ELN-TP14, ELN-CT22, ELN-V821
PDMS-tag (JP2015-026489)
ELN-V81, TPA-V81, OMC-V81

## Slide 32
Today’s topics
・ Isolation and characterization of rabbit single-chain Fv antibodies
・ Isolation and characterization of Materials-binding peptides
・ Site-specific immobilization of tagged scFvs for sensitive immuno-diagnostics

## Slide 33
Targeting domain
（scFv）
Adsorption domain
（Material-binding peptide）
Design of recombinant antibody fragments for immobilization

## Slide 34
Antibody-immobilized solid supports for immuno-diagnostics and bioprocess
Lateral-flow immunoassay
(Nitrocellulose membrane)
ELISA
（Flat polystyrene plate）
SPR sensor
(Gold thin layer)
Latex agglutination assay
(Non-porous PS latex beads)
scFv
(30 kDa)

## Slide 35: Detection of CEA in sandwich ELISA using microplate immobilized with PS-tag-fused scFv
*Solid-phase refolding

## Slide 36: Detection of Thyroid Stimulating Hormone（TSH) by scFv-PS and whole Ab
Chart: TSH concentration, ng/ml
| 100 | 25 | 6.25 | 1.5625 | 0.390625 | 9.765625E-2 | 2.44140625E-2 | 0.01
タグ付き単鎖抗体 | 3.435 | 3.41 | 3.236 | 2.037 | 0.632 | 0.215 | 0.127 | 0.11
従来の抗体 | 1.394 | 0.685 | 0.494 | 0.263 | 0.029 | 0.017 | 0.011 | 0.016
100-fold sensitivity
scFv-PS
Whole Ab
*Solid-phase refolding

## Slide 37: scFv-PM-immobilized PMMA plate for antigen detection in ELISA
Chart: Antigen concentraion, ng/ml
| 1000 | 200 | 40 | 8 | 1.6 | 0.32 | 6.4000000000000001E-2
scFv-D15 | 2.008 | 1.727 | 0.849 | 0.223 | 0.058 | 0.021 | 0.018
scFv-PM | 3.291 | 3.249 | 3.22 | 1.862 | 0.369 | 0.082 | 0.034
scFv
PMMA plate
PMMA-tag
PMMA-tag-fused scFv on PMMA plate detected the antigen with higher signal intensity.
*Liquid-phase refolding

## Slide 38
Chart: biotin-hCG concn, ng/ml
| 1000 | 250 | 62.5 | 15.625 | 3.90625 | 0.9765625 | 0.244140625 | 0.01
VHH (45ug/ml) | 0.772 | 0.869 | 0.562 | 0.265 | 0.164 | 0.087 | 0.073 | 0.066
VHH-PMMA-tag (45 ug/ml) | 3.409 | 3.455 | 3.37 | 2.863 | 1.209 | 0.602 | 0.24 | 0.076
Immobilization of Camelid VHH on PMMA plate and detection of hCG
PMMA plate
*Liquid-phase refolding

## Slide 39
Antibody-immobilized solid supports for immuno-diagnostics and bioprocess
Lateral-flow immunoassay
(Nitrocellulose membrane)
ELISA
（Flat polystyrene plate）
SPR sensor
(Gold thin layer)
Latex agglutination assay
(Non-porous PS latex beads)
scFv
(30 kDa)

## Slide 40: Application to SPR sensor
Biacore X-100
SPRセンサーの原理
Chip for SPR sensing
lazer
Prism
Gold
plastic film

## Slide 41
Chart: time(s)
SPR signals for antigen-antibody interaction was significantly improved.

## Slide 42
Antibody-immobilized solid supports for immuno-diagnostics and bioprocess
Lateral-flow immunoassay
(Nitrocellulose membrane)
ELISA
（Flat polystyrene plate）
SPR sensor
(Gold thin layer)
Latex agglutination assay
(Non-porous PS latex beads)
scFv
(30 kDa)

## Slide 43
Analyte (Serum)
Polyclonal Ab
Latex beads
C-reactive protein
(Biomarker)
Latex Turbidimetric Assay
Latex beads aggregates by immuno-interaction via antigen, and optical density quantitatively increased with antigen concentration.
Problem:
Larger amount of Antibody-immobilized latex beads have to be prepared and production cost is significantly high.
For rapid, simple and quantitative analysis of antigen
Light
Light
Notes: 現在、病気を診断する方法として、ラテックス凝集検査が広く利用されています。原理は図に示すとおりです。まず、抗体をラテックスに固定化し、バッファー中で分散します。そこに検体を加えます。検体内にバイオマーカーがあれば、抗体とバイオマーカーが抗原抗体反応起こし、その結果としてラテックスが凝集します。その際、液の濁度が上昇し、この上昇度合いを測定することで、バイオマーカーを定量します。しかし、抗体をラテックスに固定化する際、高価なWhole抗体を大量に使用するため、コストが高いことが問題となっている。

## Slide 44
Tagged scFv
PS latex
Site-specific and site-directed immobilization of scFv through the material-binding peptides
scFv
PS latex
Whole Ab
(Conventional)
PS latex
Peptide-tagged scFv
scFv
 | Whole Ab | scFv | Tagged scFv
Cost | High | Low | Low
Inactivation | Medium | High | Low
Density | Low | Medium | High
Orientation | Random | Random | Uniform
Notes: そこで、scFvのC末端に材料親和性ペプチドタグを導入しました。材料親和性ペプチドタグ融合scFvを用いることで、低コスト、低失活、高密度、高配向での固定化が可能です。

## Slide 45
Chart: scFv-PM
| 11700 | 2925 | 731.25 | 182.8125 | 45.703125 | 11.42578125 | 2.8564453125
1000ug/ml | -0.01 | 0.024 | 0.028 | 0.032 | 0.043 | 0.034 | 0.004
500ug/ml | 0.332 | 0.372 | 0.387 | 0.371 | 0.162 | 0.05 | 0.02
250ug/ml | 0.233 | 0.232 | 0.137 | 0.032 | 0.038 | 0.005 | -0.001
Chart: scFv-D10
| 11700 | 2925 | 731.25 | 182.8125 | 45.703125 | 11.42578125 | 2.8564453125
1000ug/ml | 0.317 | 0.383 | 0.41 | 0.196 | 0.064 | 0.012 | 0.009
500ug/ml | 0.407 | 0.152 | 0.044 | 0.035 | 0.024 | 0.018 | 0.01
250ug/ml | 0.007 | 0.012 | 0 | 0.001 | 0.006 | 0.011 | 0.006
Chart: D5-scFv-PM
| 10300 | 2575 | 643.75 | 160.9375 | 40.234375 | 10.05859375 | 2.5146484375
1000ug/ml | 0.322 | 0.369 | 0.387 | 0.369 | 0.122 | 0.048 | 0.025
500ug/ml | 0.376 | 0.418 | 0.344 | 0.132 | 0.041 | 0.019 | 0.009
250ug/ml | 0.13 | 0.095 | 0.049 | 0.038 | 0.038 | 0.027 | 0.025
Chart: scFv(D5)-PM
| 10300 | 2575 | 643.75 | 160.9375 | 40.234375 | 10.05859375 | 2.5146484375
1000ug/ml | 0.313 | 0.357 | 0.358 | 0.326 | 0.093 | 0.022 | 0.012
500ug/ml | 0.342 | 0.303 | 0.191 | 0.083 | 0.041 | 0.018 | 0.015
250ug/ml | 0.045 | 0.049 | 0.033 | 0.019 | 0.006 | 0.005 | 0
Chart: scFv-PM-D5
| 10300 | 2575 | 643.75 | 160.9375 | 40.234375 | 10.05859375 | 2.5146484375
1000μg/ml | 0.312 | 0.368 | 0.374 | 0.335 | 0.097 | 0.026 | 0.017
500μg/ml | 0.33 | 0.288 | 0.175 | 0.066 | 0.014 | 0 | 0.007
250μg/ml | 0.008 | 0.034 | 0.03 | 0.027 | 0.02 | 0.015 | 0.014
●：400 ng/cm2
●: 250 ng/cm2
●: 125 ng/cm2
scFv density
Terbidimetric assay of CRP by using PS latex beads with 5 different scFvs
D5-tag is more effective for improvement of dispersion of scFv-immobilized PS latex.

## Slide 46
Antibody-immobilized solid supports for immuno-diagnostics and bioprocess
Lateral-flow immunoassay
(Nitrocellulose membrane)
ELISA
（Flat polystyrene plate）
SPR sensor
(Gold thin layer)
Latex agglutination assay
(Non-porous PS latex beads)
scFv
(30 kDa)

## Slide 47
Screening and identification of nitrocellurose-binding proteins （NBPs）
4 kinds of commercially-available proteins were identified as high binders
＜Binding conditions: pH 8.0 (1×PBS), amount : 2000 ng＞
Notes: 結果をこちらに示します。親和性が低いとこちらの(a)の結果のように、CHAPS共存下にて広がり、弱い染色になります。
多くのタンパク質においてCHAPSを添加することで吸着力が弱くなりました。
しかし、リゾチーム、ラクトフェリン、ヘモグロビン、ヘモシアニン、コンカナバリンＡでは0.2%CHAPS共存下においても比較的スポット径の広がりが小さく、NC膜に親和性が高いことが示唆されました。

## Slide 48
Conjugation of scFv with NBPs
◆ Thiol-maleimide coupling
1:100
1:100
NBPs
scFv-NPBs
iminothiolane
SMCC
Coupling reaction
Notes: 使用したscFvは、CRP抗原に対して結合性を有するanti-CRP scFvを用いました。
NC親和性タンパク質との結合方法としてマレイミドカップリング反応を用いました。反応スキームはこちらに示す通りです。

## Slide 49
Lateral-flow immunoassay using scFv-NBPs
Immobilization
Ab Conc：0.5 mg/ml
Spot volume：2 μl
Sample application
Ag conc：0～28.4 pfu/ml
Latex conc：0.0172％
Total volume：100 μl
10 min
Signal detection
・scFv
・scFv-NBP-1
・scFv-NBP-2
・Whole Ab
Notes: 次に、抗原検出限界濃度を検討することで、どの程度検出感度が向上しているのかの確認を行いました。
固定化はそれぞれの最適条件にて行い、抗原濃度を0～28.4pfu/mlに調製し、抗原検出を行いました。また、従来法に使用されているWhole抗体との比較を行いました。

## Slide 50
Lateral-flow immunoassay using scFv-NBPs
Inactivated Flu B virus
Virus conc : 28.4 ～0 pfu/ml
scFv-NBP-1
scFv-NBP-2
scFv
Whole Ab
scFv-NCBs were 280-fold sensitive than scFv
scFv-NCBs were 70-fold sensitive than whole Ab.
Notes: 結果です。
シグナル強度の比較より、scFv-LF,scFv-ConAはscFvの280倍低濃度の抗原を、また、従来抗体の70倍低濃度の抗原を検出出来ました。

## Slide 51: Summary
The methodology for identification of antigen-specific rabbit scFvs was established.
The methodology for identification and characterization of materials-binding peptides was established.
Materials-binding peptides improve adsorption density, orientation and remaining activity of target proteins in adsorption states.
Thus, the materials-binding peptides/proteins developed in this study will be considerably useful for immobilization of target protein and they will be applicable to immuno-diagnostics.

## Slide 52
Acknowledgements
・ Prof. Jun-ichi Horiuchi (Kyoto Institute of Technology)
・ Prof. Michimasa Kishimoto (Kyoto Institute of Technology)
・ Biochemical Engineering Lab members, KIT
Our researches were partially supported by JSPS, JST, NEDO and companies.