## Slide 1
Chart: pH
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
Washing with milli-Q water | 52.3871 | 49.8956 | 50.8896 | 54.7686 | 62.8366 | 61.4641 | 61.0326 | 60.9956 | 52.7591 | 55.2146 | 45.9331 | 33.3601 | 35.9761 | 41.1926
Washing with TBST | 46.2288 | 46.2033 | 43.9923 | 47.6253 | 43.4308 | 37.7268 | 37.7583 | 37.5388 | 39.5203 | 42.5023 | 34.5093 | 24.4653 | 25.8533 | 35.1908
Characterization of adsorption and residual activity of antibodies immobilized on the surface of NC membrane
Conclusion
SCEJ 90th Annual Meeting
Introduction
Objective
Materials and methods
Results and discussion
PA131
Characterization of adsorption and residual activity of antibodies on the surface of nitrocellulose membrane irradiated by oxygen plasma
(Kyoto Inst. Tech.) ○(Stu) Manami Takata・ (Stu) Yuki Nagahisa ・(Toyo Roshi) Toshihiro Nakanishi・(Toyo Roshi) Yoshihiko Inaba・ (Kyoto Inst. Tech.) (Reg) Jun-ichi Horiuchi・(Reg) Yoichi Kumada *
Development of NC membranes suitable for antibody immobilization by oxygen plasma treatment
・Hydrophobic interaction
・Hydrogen bonding
・Electrostatic interaction etc
Nitrocellulose membrane (NC membrane)
In this study, we focused on oxygen plasma treatment, which is one of the popular surface modification methods
Porous and hydrophobic membrane used for antibody immobilization in immunochromatography
The adsorption and residual activity of monoclonal antibody on the oxygen plasma-irradiated NC membrane were investigated.
Ex) If the adsorption condition is not appropriate,
NC membrane
After adsorption
Conformational changes
Desorption
◆ Adsorption characterization
◆ Residual activity check
・CBB staining and decolorization ・Washing with milli-Q water ・Scanning by Image J
・Blocking with 2% BSA-TBS
・Reaction with Bt-hCG (10 ng/mL)
・Reaction SA-AP
・Enzymatic reactions with BCIP/NBT
・Scanning by Image J
SA-AP
BCIP/NBT
Bt-hCG
Antibody
NC membrane
protein
NC membrane
CBB staining
Oxygen plasma irradiation
◆ Spotting and washing
Spotting the sample
solution on NC
membrane(2 μL)
Washing with mili-Q water (10 min)
Washing with TBST (10 min)
Washing methods
Adsorption characterization
Residual activity check
Materials
Methods
酸素プラズマ照射ニトロセルロース膜に対する抗体の吸着特性
及び残存活性の評価
◆ Oxygen plasma conditions
◆NC membranes
Membrane for Immunochromatography IAB135-EX (Advantec)
◆Antibodies
Mouse IgG (Fujifilm WAKO)
Anti-hCG Mouse mAb(4G2) (Advantec)
◆Antigen
Human Chorionic Gonadotropin(hCG) (Merck)
◆Buffer
✔ Characteristics of antibody adsorption and residual activity on NC membrane were clarified.
✔ It was suggested that the surface properties of NC membrane were changed by oxygen plasma treatment under the low pressure condition.
✔ Oxygen plasma irradiation has a potential to improve antigen-binding activities of antibodies after adsorption.
pH | 1-3 | 4 | 5-6 | 7-8 | 9-12 | 13-14
Buffer | Gly-HCl | Acetate | MES | Tris-HCl | Gly-NaOH | KCl-NaOH
Component | Concentration
Antibody | 0～400 µg/mL
Buffer | 50 mM
◆Sample solution
・Treatment of NC membranes at 10 Pa improved the residual activity of monoclonal antibody after adsorption.
・Antigen-binding signals were increased with concentrations of antibody spotted.
・Washing with TBST significantly dissociated the adsorbed antibodies at pH 5-8 .
・Antigen-binding activities of antibodies that were adsorbed at neutral pH
(pH5-8) were relatively maintained at high levels.
・It was found that adsorbed antibodies were inactivated under the acidic and alkaline conditions.
Antigen-binding activities of monoclonal antibodies adsorbed on NC membranes irradiated by oxygen plasma
Effect of antibody concentration on antigen-binding activity
〇High water absorption property
〇High adsorption capacity of proteins
△Proteins might be strongly interacted on the surfaces by multiple types of interactions such as
Chart: pH
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
Washing with TBST | 50.1381 | 93.0721 | 105.0246 | 136.0301 | 99.8296 | 108.9481 | 113.8761 | 129.9176 | 116.2721 | 113.1921 | 80.5131 | 54.3491 | 29.4676 | -0.21343
Adsorption Residual activity
Chart: Oxygen plasma conditions
| non-treatment | 1 | 2 | 3 | 4
pH7 | 76.7072 | 96.9082 | 65.4257 | 94.5817 | 90.6342
C
T
Chart: antibody conc. (μg/ml)
| 400 | 200 | 100 | 50 | 25 | 12.5 | 0
non-treatment | 60.5054 | 36.2089 | 29.1649 | 18.2564 | 6.6079 | 0.99786 | -1.0216
Oxygen plasma treatment(condition1) | 92.5226 | 75.4706 | 49.5676 | 28.8466 | 11.2561 | 3.7771 | -1.1724